Автоматизированный анализ распределения диаметров и неравномерности расположения волокон в композитах с непрерывным армированием по СЭМ-снимкам поперечных сечений

Наконечный Е.И.1, Хохлов А.В.2, Галышев С.Н.3, Атанов Б.И.3, Орлов В.И.3

1 МГУ имени М.В. Ломоносова (физический факультет), Москва, Россия

2 НИИ механики МГУ имени М.В. Ломоносова, Москва, Россия

3 Институт физики твердого тела им. Ю.А. Осипьяна РАН, Черноголовка, Россия

E-mail: egornakonecnyj7972@gmail.com

Разработаны методика и алгоритмы для обработки данных сканирующей электронной микроскопии (СЭМ) поверхностей разрушения композитов с параллельным армированием. Разработанный программный комплекс (ПК) обеспечивает сбор полной статистики по распределению волокон по диаметрам и площадям в поперечном сечении образца, выявление кластеров и количественную оценку плотности распределения волокон по сечению (вариаций их объемной доли) и характеристик его неравномерности. Отработка и верификация ПК проводилась на нескольких сериях СЭМ-снимков шлифов поперечных сечений углеалюминиевой проволоки с матрицей из технически чистого алюминия или сплава Al-0.5Bi, непрерывно армированной углеродными волокнами. Проволока изготовлена в ИФТТ РАН, ее диаметр – 300 мкм, объемная доля волокон менялась от 40 до 60%. Разработанный ПК полезен как инструмент для технического контроля качества в процессе производства композитных материалов и позволяет получить ценную информацию для понимания строения и моделирования поведения однонаправленных композитов.

Ключевые слова: однонаправленные композиты, углеалюминиевые композиты, СЭМ, распределение диаметров волокон, неравномерность распределения волокон по сечению

Automated analysis of diameter distribution and uneven fiber distribution in continuously reinforced composites based on SEM images of cross sections

Nakonechnyi Ye.I. 1, Khokhlov A.V. 2, Galyshev S.N. 3, Atanov B.I. 3, Orlov V.I. 3

1 Faculty of Physics, Lomonosov Moscow State University, Moscow, Russia;

2 Institute of Mechanics, Lomonosov Moscow State University, Moscow, Russia;

3 Osipyan Institute of Solid State Physics RAS, Chernogolovka, Russia;

E-mail: egornakonecnyj7972@gmail.com

Methods and algorithms have been developed for processing scanning electron microscopy (SEM) data of parallel-reinforced composite fracture surfaces. The developed software package (SP) provides complete statistics on the distribution of fibers by diameter and area in the cross section of the sample, identification of clusters, and quantitative assessment of the density of fiber distribution across the cross section (variations in their volume fraction) and characteristics of its unevenness. The software package was tested and verified on several series of SEM images of cross sections of carbon-aluminum wire with a matrix of pure aluminum or Al-0.5Bi alloy, continuously reinforced with carbon fibers. The wire was manufactured at the Osipyan Institute of Solid State Physics RAS, its diameter is 300 μm, and the volume fraction of fibers varied from 40 to 60%. The developed software is useful as a tool for technical quality control in the production of composite materials and provides valuable information for understanding the structure and modeling the behavior of unidirectional composites.

Keywords: unidirectional composites, carbon-aluminum composites, SEM, fiber diameter distribution, uneven fiber distribution across the cross-section